**SECTION 09 65 19.23 – VINYL TILE FLOORING**

1. **GENERAL**
   1. SUMMARY
      1. SECTION INCLUDES:
         1. Glue Down Luxury Vinyl Tile (LVT)
         2. Adhesives
      2. RELATED SECTIONS
         1. Section 03300 - Cast-In-Place Concrete Floor substrate requirements.
         2. Section 06200 - Rough Carpentry: Floor substrate requirements.
   2. REFERENCES
      1. American Concrete Institute (ACI):
         1. ACI 302.2R - Guide for Concrete Slabs that Receive Moisture-Sensitive Flooring Materials
      2. American Society for Testing and Materials (ASTM):
         1. ASTM D2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Flooring Surfaces as Measured by the James Machine.
         2. ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.
         3. ASTM E648 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.
         4. ASTM E662 - Standard Test Method for Specific Optical Density of Smoke Generated by Solid Materials.
         5. ASTM F137 - Standard Test Method for Flexibility of Resilient Flooring Materials with Cylindrical Mandrel Apparatus.
         6. ASTM F141 - Standard Terminology Relating to Resilient Floor Coverings
         7. ASTM F373 – Standard Test Method for Embossed Depth of Resilient Floor Covering
         8. ASTM F386 – Standard Test Method for Thickness of Resilient Flooring Materials Having Flat Surfaces
         9. ASTM F410 – Standard Test Method for Wear Layer Thickness of Resilient Floor Coverings by Optical Measurement
         10. ASTM F710 - Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring.
         11. ASTM F925 - Standard Test Method for Resistance to Chemicals of Resilient Flooring.
         12. ASTM F970 - Standard Test Method for Static Load Limit.
         13. ASTM F1482 – Standard Practice for Installation and Preparation of Panel Type Underlayments to Receive Resilient Flooring.
         14. ASTM F1514 - Standard Test Method for Measuring Heat Stability of Resilient Flooring by Color Change.
         15. ASTM F1515 – Standard Test Method for Measuring Light Stability of Resilient Flooring by Color Change
         16. ASTM F1700 – Standard Specification for Solid Vinyl Tile
         17. ASTM F1869 - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride
         18. ASTM F1914 - Standard Test Methods for Short-Term Indentation and Residual Indentation of Resilient Floor Covering.
         19. ASTM F2055 – Standard Test Method for Size and Squareness of Resilient Floor Tile
         20. ASTM F2199 - Standard Test Method for Determining Dimensional Stability of Resilient Floor Tile after Exposure to Heat.
         21. ASTM F2419 – Standard Practice for Installation of Thick Poured Concrete Underlayments and Preparation of the Surface to Receive Resilient Flooring.
         22. ASTM F2471 – Standard Practice for Installation of Thick Poured Lightweight Cellular Concrete Underlayments and Preparation of the Surface to Receive Resilient Flooring.
      3. National Fire Protection Association (NFPA)
         1. NFPA 80 – Fire Safety Code.
         2. NFPA 253 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Energy Source.
         3. NFPA 255 - Standard Test Method for Surface Burning Characteristics of Building Materials.
         4. NFPA 286 - Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth.
      4. Resilient Floor Covering Institute (RFCI)
         1. Recommended Work Practices for Removal of Resilient Floor Coverings
      5. Underwriters Laboratories (UL) Environment
         1. UL 410 – Slip Resistance of Floor Surface Materials
   3. SUBMITTALS
      1. General: Submittals must be submitted the under provisions of Section 01300.
      2. Product Data: Manufacturer's published documents on each product to be used, including:
         1. Technical Data Sheet
         2. Installation Instructions
         3. Maintenance Guide
         4. Product Warranty
         5. AVA Material Usage Guide Technical Bulletin
         6. AVA Wet Area Installation Technical Bulletin
         7. Additional Technical Documents
            1. Relevant test reports
            2. Relevant technical bulletins
            3. Additional recommendations or requirements
      3. Selection Samples: For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
      4. Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square or one full tile, representing actual product, color, and patterns.
   4. QUALITY ASSURANCE
      1. Qualifications:
         1. Installer Qualifications: Installer must be a professional, licensed and experienced installer. Installer must have familiarity with both the type, size and format of the product.
         2. Manufacturer’s Qualifications
            1. Manufacturer must provide remote and field technical support and service prior to, during and following installation, as necessary.
      2. Mock-Up:
         * 1. Provide a mock-up for evaluation of product, surface preparation techniques and installation workmanship.
           2. Do not proceed with remaining work until size, color, thickness, sheen and workmanship are approved by Architect, End-User and/or other stakeholders.
           3. Maintain mock-up area as required in accordance with the Product Data to produce acceptable work.
   5. DELIVERY HANDLING & STORAGE
      1. Ordering: Comply with manufacturer’s ordering and lead time requirements to avoid construction delays.
      2. Receiving Material: Remove all plastic and strapping from product after delivery. Confirm that the flooring product color, style, quantity and lot numbers are all correct. Carefully check all materials for shipping damage and note all damage on the bill of lading before accepting the delivery. Material accepted with visible shipping damage that is not reported on the bill of lading is not covered under warranty. Ensure that the adhesive intended for installation is approved for use with the flooring product.
      3. Storage: The floor covering, adhesive and accessories must be stored in dry indoors conditions between 40°F to 90°F (4°C to 32°C). Do not store outside (even in containers) and do not stack pallets. Deliver all materials to the installation location in its original packaging with labels intact.
      4. Acclimation: The temperature for the installation must match the temperature when the product will be in use (in-service temperature) and be constant (± 5°F). In addition, ambient temperatures must be between 60°F (16°C) and 80°F (27°C) for ≥ 48-hours before, during and after the installation. The ambient relative humidity must be between 35% and 65% and ≥ 10°F above dew point (dew point calculators are available on the internet), or adhesive working and/or curing times will be severely affected.
   6. PROJECT CONDITIONS
      * 1. Environmental Conditions: Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer in accordance with the Product Data. Do not install products under environmental conditions outside manufacturer's absolute limits.
      1. WARRANTY
         1. Project Warranty: Refer to Conditions of Contract for project warranty provisions.
         2. Manufacturer’s Warranty:
            1. When used in accordance with the Product Data and the AVA Material Usage Guide, AVA ORBT shall comply with all written specifications and be free from Manufacturing Defects and wear-through for the following periods:

Residential: Lifetime from the date of purchase.

Commercial: Twenty (20) years from date of purchase.

1. **PRODUCTS**
   1. PRODUCT MANUFACTURERS
      1. Acceptable Manufacturer:
         1. Novalis Innovative Flooring

200 Munekata Dr SE

Dalton, GA 30721

P: 877.861.5292  
E: sales@avaflor.com

Web: www.avaflor.com

* 1. SUBSTITUTIONS
     + 1. \*\* NOTE TO SPECIFIER \*\* Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.
     1. Substitutions: Not permitted.
     2. Requests for substitutions will be considered in accordance with provisions of Division 01.
  2. PRODUCT DIMENSIONS

\*\* NOTE TO SPECIFIER \*\* Delete products and sizes not required.

* + 1. Product: AVA ORBT Luxury Vinyl Tile (LVT) as manufactured by Novalis Innovative Flooring.
       1. Sizes (all sizes nominal):
          1. 6 inches by 48 inches by 0.98 inches (152.39 mm by 1212.85 m by 2.5mm)
          2. 24 inches by 24 inches by 0.98 inches (609.6 mm x 609.6mm x 2.5mm)
  1. PRODUCT COLOR

\*\* NOTE TO SPECIFIER \*\* Delete colors not required.

* + 1. Black Knight
    2. Blue Tide
    3. Crushed Ice
    4. Knockout Orange
    5. Lemon Twist
    6. Lucky Shamrock
    7. Mariner Blue
    8. Purple Bliss
    9. Spicy Sangria
    10. Star Dust
    11. Stormy Seas
    12. Very Berry
  1. PHYSICAL CHARACTERISTICS

\*\* NOTE TO SPECIFIER \*\* Delete surfaces not required.

* + 1. Surface: Textured With Straight Edge
    2. ASTM F1700 – Solid Vinyl Tile:
       1. Classification: Class III, Type B
       2. ASM F2055 – Size: Passes, ± 0.4 mm
       3. ASTM F387 – Thickness of Resilient Flooring: Passes, ± 0.13 mm
       4. ASTM F410 – Wear Lay Thickness: Passes, ≥ 0.5 mm
       5. ASTM F2055 – Squareness: Passes, ± 0.25 mm
       6. ASTM F1914 – Residual Indentation: Passes, <0.2 mm
       7. ASTM F137 – Flexibility: Passes, 25.4 mm mandrel
       8. ASTM F2199 – Dimensional Stability: Passes, <0.05 mm/ lin. ft.
       9. ASTM F925 – Chemical Resistance: Passes ASTM F1700 Requirements
          1. White vinegar (5% Acetic Acid) - Passes.
          2. Rubbing Alcohol (70% Isopropyl Alcohol) - Passes.
          3. Lye (5% Sodium Hydroxide) - Passes.
          4. Hydrochloric Acid (5% HCI) - Passes.
          5. Sulfuric Acid (5%H2SO4) - Passes.
          6. Household Ammonia (5% Ammonia) - Passes.
          7. Disinfectant Cleaner (5% Active Phenol) - Passes.
          8. Household Bleach (5.25% NaOCl) - Passes.
          9. Unleaded Gasoline - Passes.
          10. Kerosene - Passes.
          11. Olive Oil - Passes.
       10. ASTM F1514 – Color Heat Stability: Passes, ΔE<8
       11. ASTM F1515 – Color Light Stability: Passes, ΔE<8
       12. ASTM F970 – Static Load Limit: Passes, ≤ 0.5 mm indent, 250 lbs.
    3. ASTM E648 (NFPA 253) – Critical Radiant Flux: Class I, > 0.45 W/cm2
    4. ASTM E662 (NFPA 258) – Smoke Density: Passes, <450
    5. ASTM D2047 / UL 410 – Slip Resistance: >0.5 SCOF
    6. ASTM E492 / E989 – Impact Insulation: IIC 52 w/ Novalis 22-SCU (6 in. Concrete)
    7. ASTM E90 / E413 – Sound Transmission: STC 54 w/ Novalis 22-SCU (6 in. Concrete)
    8. ASTM E2179 – Delta Impact Insulation: ΔIIC 23 w/ Novalis 22-SCU (6 in. Concrete)
  1. PRODUCT ADHESIVE

\*\* NOTE TO SPECIFIER \*\* Delete adhesive not required.

* + 1. Only Novalis approved adhesives shall be used when installing ORBT.
       1. Novalis NV-GLU Acrylic Adhesive
       2. Gold Series MW 3012 MS Resilient Flooring Adhesive.

1. **EXECUTION**

\*\* NOTE TO SPECIFIER \*\* Revise articles below to suit specific project requirements.

* 1. MANUFACTURERS INSTRUCTIONS
     1. Compliance: Review and comply with manufacturer’s Product Data, including technical data sheets, installation instructions, maintenance documents, warranty information, technical bulletins and all other written technical documents, specifications and communications.
  2. EXAMINATION
     1. Site Verification of Conditions:
        1. Verify substrate conditions, which have been previously installed under other sections, are acceptable for product installation in accordance with manufacturer’s Product Data.
        2. Do not begin installation until all substrates have been properly tested and prepared in accordance with the ORBT Product Data and applicable ASTM, ACI, NWFA and RFCI standards.
        3. If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.
  3. PREPARATION
     1. Cleaning: Clean surfaces thoroughly prior to installation.
     2. Substrate Preparation: Prepare surfaces in accordance with substrate preparation requirements published in the ORBT Product Data.
  4. INSTALLATION
     1. Flooring Installation: Install materials in accordance with installation instructions published in the ORBT Product Data.
     2. Traffic Limits: No traffic, cleaning, finishing or placement of furniture should occur in accordance with adhesive traffic limits published in the adhesive Product Data.
     3. Initial Maintenance: Once adhesive has cured, perform initial maintenance in accordance with initial maintenance instructions published in the ORBT Product Data.
  5. MAINTENANCE
     1. Daily Maintenance: Long-term care and maintenance must be performed in accordance with daily and routine maintenance instructions published in the ORBT Product Data.
  6. PROTECTION
     1. Temporary Floor Protection: Protect installed products until completion of project in accordance with flooring or material protection requirements published in the ORBT Product Data.
     2. Repair: Touch-up, repair or replace damaged products before Substantial Completion.
     3. Permanent Floor Protection: Ensure furniture feet/bottom, glides and chair casters dimensions and materials are in accordance with floor protection requirements published in the ORBT Product Data prior to Substantial Completion.

**END OF SECTION**